# earth4Earth                                                                                                No.: DoP-UK-BR-N10a-2024-01

# Declaration of Performance

Unique identification code of the product-type: Clay Masonry Unit (Compressed Earth Brick)

Intended use or uses of the construction product, in accordance with the applicable harmonised technical specification, as foreseen by the manufacturer: For use in facing and rendered masonry, low-rise load-bearing or non-load-bearing masonry low risk structures, including internal linings and partitions, in accordance with EN 771-1.

Use in unprotected masonry structure

Registered office:

earth4Earth Technology Ltd, 85 Great Portland Street, London, England, W1W 7LT

Attestation of Conformity System 4

Under System 4, the manufacturer is responsible for the determination of product type, factory production control, and testing in accordance with the relevant harmonised technical specification. The notified certification body SGS-CSTC Standards Technical Services Co. Ltd has carried out the product testing and has issued the corresponding UKCA certificate.

Declared Performance:

| Essential Characteristics | Performance | Harmonised Technical Specification |
| --- | --- | --- |
| Dimensions and tolerance (mm) | 215 x 102.5 x 65 | BS EN 771-1:2011+A1:2015 |
| Tolerance | T2 | BS EN 771-16 |
| Configuration | Solid unit | BS EN 771-1 |
| Declared Dry Density (kg/m3) | 1850 | BS EN 771-13 |
| Flatness of bed faces, maxmum deviation (mm) | 0.15 | BS EN 771-20 |
| Plane parallelism, maxmum deviation (mm) | 0.57 | BS EN 771-16 |
| Declared Compressive strength (MPa) | 10 | BS EN 771-1:2011 |
| Range Category | R2 | BS EN 771-1 |
| Flexural strength (N/mm2) | 0.2 | BS EN 771-1 |
| Bond strength fixed (N/mm²) | 0.15 | BS EN 998-2:2010 |
| Active soluble salts | S2 | BS EN 771-1 |
| Reaction to fire | A1 | EN 13501-1 |
| Water absorption (%) | ≤ 16% | BS EN 771-1 |
| Water vapour permeability kg/(s∙m∙Pa) | 1.19E-11 | BS EN ISO 12572 |
| Initial rate of water absorption kg/(m2*min) | 1.54 | EN 771-1 |
| Thermal conductivity (λ10,dry) W/mK | 0.9 | EN 1745 |
| Durability against freeze-thaw | F1 (50) | BS EN 771-1 |
| Specific heat capacity J/(g·K) | 0.8392 J/(g·K) | BS EN 1745-2020 |
| Elastic modulus MPa | 1531 | ASTM C469/C469M - 22 |
| Dangerous substances | fully recyclable | 2003/33/EC |

The performance of the product identified above is in conformity with the declared performance.

This declaration of performance is issued, in accordance with the Construction Products Regulation 2011 (retained EU law EUR 2011/305) as amended by the Construction Products (Amendment etc.) (EU Exit), Regulations 2019 and Construction Products (Amendment etc.) (EU Exit), Regulations 2020 under the sole responsibility of the manufacturer identified above.

Signed for and on behalf of the manufacturer by:
Name: Lei Zhang

Position: Director and R&D Manager
Place and date of issue: 07/2025
Signature: